## Slide 1
Yutao Xing
Instituto de Física, Universidade Federal Fluminense
Magnetismo
(experimental)
Notes: 1

## Slide 2
PARTE TEORIA (PROF. Daniel Rocco)
Paramagnetismo
Diamagnetismo
Ferromagnetismo
Antiferromagnetismo
Ferrimagnetismo
Superparamagnetismo

## Slide 3
Parte experimental
Magnetismo conectado conosco
3
Notes: 3

## Slide 4
Pode escapar de magnetismo?
4
PÓLO NORTE
PÓLO SUL
Notes: 4

## Slide 5
Utilização do campo de terra
5
bússola
Notes: 5

## Slide 6
Como ela funciona?
6
Interação entre imã e campo magnético:
A
A
Notes: 6

## Slide 7
7
Por que tem interação entre imã e ferro?
Interação: imã e ferro
Domínio !
Notes: 7

## Slide 8
8
Perguntas:
Por que não tem interação entre imã e cobre?
Por que a imã na porta de geladeira não cai?
Interação: imã e ferro
Notes: 8

## Slide 9
9
Material magnética dura:
NdFeB
Material magnética macia:
FeNi
Material ferromagnética:
Pergunta: Qual é diferença magnética entre FeNi e Cu?
Notes: 9

## Slide 10
10
Por que depois de tirar o campo, os momentos magnéticos não voltam para direção e sentido anterior?
Material ferromagnética:
Anisotropia:
Anisotropia cristalina
Anisotropia de forma
Notes: 10

## Slide 11
11
Utilização dos domínios
Notes: 11

## Slide 12
12
Utilização dos domínios
Notes: 12

## Slide 13
13
Utilização dos domínios
Notes: 13

## Slide 14
1.27 × 107 m
ww.mathworks.com
0.22 m
0.7 × 10-9 m
Fullerenes C60
12,756 Km
22 cm
0.7 nm
10 millions times smaller
1 billion times smaller
www.physics.ucr.edu
Nanomagnetismo: uma nova era
O que é nano? 1nm = 1x 10-9 m Diâmetro de cabelo: 70 µm = 70 000 nm

## Slide 15
15
Nanomagnetismo: uma nova era
Nano Material:
0D: nanopartículas
1D: nanofios (nanotubo de carbono)
2D: filme finos
3D: materiais nanocristalinas.
Notes: 15

## Slide 16
Size comparable to quantum mechanical length scales
  e.g. mean free path, coherence length, etc.
  quantum effects
Number of atoms is limited
no classical thermodynamics
Surface effect
  Dimension
Fraction of surface
number of surface atoms > number of core atoms
16
Nanomagnetismo: as diferenças
Notes: 16

## Slide 17
New physics phenomena I
Giant magnetoresistance (GMR)
Wide applications:
2007 Nobel prize
17
Notes: This is nano multilayres thickness is close to the lamda as I mentioned. Another example is the spin torque effect
17

## Slide 18
Question:
Why other people did not discover GMR before these two researchers since many people were doing research with thin films?
Answer:
Dimensions!
  Thickness of the thin films < mean free path of the free electrons
18
New physics phenomena I
Notes: 18

## Slide 19
New physics phenomena II
Spin torque effect
Magnetic moment can be flipped by spin-polarized current.
19
Notes: The third example I would like to give is the study of carbon nanotubes
19

## Slide 20
New physics phenomena II
Spin torque effect
20
Question:
Why other people did not discover STE before?
Answer:
Dimensions!
Very high Current density!!
Only with very good e-beam lithography can they make the sample !
Notes: The third example I would like to give is the study of carbon nanotubes
20

## Slide 21
New physics phenomena III
Carbon nanotubes
From Prof. Paul Midgley, Cambridge
Single domain Fe particle inside !
Carbon nanotube can be aligned by external magnetic field.
With nano contacts, transport properties of a single carbon nanotube can be studied.
21
Notes: Because the nanosience is so interesting, the researchers are trying different methods to make nano scaled materials
21

## Slide 22
How to prepare nano-scaled materials?
22
?
Notes: These are the methods to prepare the nano materials. For the research of physics, I would like to focus on the following topics,
22

## Slide 23
23
?
How to prepare nano-scaled materials?
Notes: These are the methods to prepare the nano materials. For the research of physics, I would like to focus on the following topics,
23

## Slide 24
24
How to prepare nano-scaled materials?
Filme finos:
Técnicas de deposição:
Sputtering
MBE
Ablação por laser
......
Nano partículas:
Método química
Método física
......
Notes: These are the methods to prepare the nano materials. For the research of physics, I would like to focus on the following topics,
24

## Slide 25
25
How to prepare nano-scaled materials?
Ablação por laser
Notes: These are the methods to prepare the nano materials. For the research of physics, I would like to focus on the following topics,
25

## Slide 26
Introduction to the system
Installed in 2011
Base pressure: 4 x 10-7 Torr
(Pressure can be reached in one hour)
Power of laser: 500 mJ
Pulse of laser: 10 pulses/second
Notes: we can find the IV curves seperated into two different groups: above Tg and below Tg. With the above data ,we can not conclude that the spontaneous vortices are related with the Co nanoparticles in the sample, In order to clarify this doutb, we did the following experiments:

## Slide 27
Plasma of Ni

## Slide 28
Plasma of Tin

## Slide 29
Sample preparation
Thin films: in vacuum
Nanoparticles: in Ar with a pressure of 1 torr

## Slide 30
Ni nanoparticles

## Slide 31
Ni nanoparticles

## Slide 32
Aplicação das nanoparticulas magnéticas
Cancer treatment
Drug delivery
Nanoparticulas:
Superparamagnetic

## Slide 33
33
Thin film to nano patterns
Notes: These are the methods to prepare the nano materials. For the research of physics, I would like to focus on the following topics,
33

## Slide 34
What is lithography?
34
Notes: 34

## Slide 35
Photolithography
35
Notes: 35

## Slide 36
Photolithography
36
Notes: 36

## Slide 37
Photolithography
37
Notes: 37

## Slide 38
Resolution of Photolithography
38
Resulution: ~1 μm
Notes: 38

## Slide 39
E-beam lithography
39
Question:
How to improve the resolution of lithography?
Answer:
Use beams with much shorter wave length!
Rayleigh Criterion: θR = 1.22 λ/D
Notes: 39

## Slide 40
Visible light:
400 ~ 700 nm
Shoter:
Ultraviolet <400 nm
X-ray 0.01 nm ~ 10 nm
Quantum mechanics:
  λ = h/P
40
Wavelength of different beams
Electron beams: (energy: 10 KeV ~200 KeV)
  λ : 0.002 nm ~ 0.01 nm
Notes: 40

## Slide 41
Requirements for research with EBL
High quality thin films
  basic requirement, scientific results directly depend on the film quality.
Good EBL
determines the quality of the pattern.
Characterization techniques
  to study the properties of the obtained patterns
  e.g. TEM
41
Notes: In this case I would like to show the facilities at CBPF which can be used for nanoscience. The first one is
41

## Slide 42
E-beam lithography system
42
Notes: 42

## Slide 43
Process of E-beam lithography
43
Two different processes :
Lift-off (bottum-up)
Etching (top-down)
Notes: 43

## Slide 44: Etching process
substrate
deposition
substrate
Sample layer
E-beam
lithography
substrate
photoresist
substrate
Spin-coating
etching
substrate
substrate
remove
resist
44
Notes: 44

## Slide 45: Lift-off
substrate
Spin-coating
substrate
E-beam
lithography
deposition
substrate
substrate
remove
resist
45
substrate
Notes: 45

## Slide 46: E-beam lithography
 spin-coating of resist (340 nm thickness)
class 100 clean bench
Notes: Should say I was working there

## Slide 47: E-beam lithography
 Ar plasma-etch
Oxford Plasmalab 80+ reactive ion etching system

## Slide 48: E-beam lithography
Question:
Positive or negative resist? Why?
Answer:
we have to use LESS machine time!!

## Slide 49
The dusts in the air are much bigger than the patterns!
EBL need Cleanroom

## Slide 50
EBL need Cleanroom

## Slide 51
EBL need Cleanroom

## Slide 52
DEMUX device J. Degenhardt, University of Duisburg, Germany
Applications – Electrical Engineering

## Slide 53
Air bridges F. Robin, ETH Zürich, Switzerland
Applications – Electrical Engineering
Applications – Electrical Engineering

## Slide 54
Electrical nm-contact fingers for Carbon Nanotube transport measurement Adrian Bachthold, University of Basel, Switzerland
Applications – Physics
Applications – physics

## Slide 55
Al-nanobridge used as a tunneling contact (after mechanical break)
M. Goffman, CEA Saclay, France E. Scheer, University of Konstanz, Germany
Applications – physics

## Slide 56
Nanostructure array for Magnetoelectronics - sub--squares covering 5mm2, M. Fraune, Technical University of Aachen, Germany
Applications – Physics
Applications – physics

## Slide 57
Nanostructure arrays for Magnetoelectronics - 30nm Quantum dots
University of Bielefeld, Germany
Nanostructure arrays for Magnetoelectronics - 200nm-lines covering 5mm2
M. Fraune, Technical University of Aachen, Germany)
Applications – Physics
Applications – physics

## Slide 58
Nano-Structures in ferromagnetic digital alloy G. Schmidt et al. University of Würzburg, Germany
Applications – Physics
Applications – physics

## Slide 59
Double Quantum dot structure in free standing GaAs/AlGaAs E.M. Weig, LMU Munich, Germany
Applications – Physics
Applications – physics

## Slide 60
Nano-Hallbar G. Schmidt et al. University of Würzburg, Germany
Applications – Physics
Applications – physics

## Slide 61
Magnetic resonance sensor G. Schmidt et al., University of Würzburg, Germany
Applications – Physics
Applications – physics

## Slide 62
Ballistic transport device
J. Appenzeller, Technical University of Aachen, Germany
Quantum Effects in Superconductor/Hybrid Devices - Electronic transport studies in
InGaAs/InP heterostructure J. Appenzeller, Technical University of Aachen, Germany
Applications – Physics
Applications – physics

## Slide 63
Photonic Crystal membrane nano-cavity with InAs quantum dot
as single photon source, Wen-Yen Chen, NCU, Taiwan
Applications – Optoelectronics / Optics

## Slide 64: Applications – Mater. Science / Process technology
Metallic Air Bridge
Tatjana Borzenko et al., University of Würzburg, Germany
Air bridge fabrication offshoot
„fruit on a table“
Tatjana Borzenko et al.,
University of Würzburg, Germany
Notes: Clumsy creatures appeared during process development of air bridge!
Siehe pdf Dokument für ausführliche Beschreibung!

## Slide 65
Replication of structures etched in Si, K. Otte, IOM Leipzig, Germany
Applications – Mater. Science / Process technology
Applications – Mater. Science / Process technology

## Slide 66
Exposure
at 10 keV !
6nm lines exposed in HSQ resist at 10 keV only, D. Lucas, Raith inhouse
Exposure
at 10 keV !
6 nm
Applications – Ultra High Resolution Lithography

## Slide 67
Pyramid Retro Reflectors T. Dillon, University Delaware, USA
Applications – 3D Lithography
Applications – 3D Lithography

## Slide 68
3D-Lithography tests for MEMS T. Dillon, University Delaware, USA
Applications – 3D Lithography
Applications – 3D Lithography

## Slide 69
3D-Lithography 1: TIFF-Image 2: AFM-image of 3D-pattern, developped in PMMA 3: 3D-view of AFM-image in 2 to visualize height profile H. Raith, Raith inhouse
3
1
2
Applications – 3D Lithography
Applications – 3D Lithography

## Slide 70
Welcome to join us!